Solvent accessible surface area (SASA)

In order to study the drug release of polymer prodrugs, we compare the Solvent accessible surface of active points (Amide) in aggregate (contains 24 chains) and 1 chain (in octanol and in same calculate condition (water, WF and ions, same concentration of GemPi1kda)

1. 1chain in octanol (jarre, 6h)

:~/GemPi1kDa/byrd03/octanol/Take6_ok/test_sasa
~/ProDrug/GemPi1kDa/byrd03/solution/Gem24/trajectory/1chain_octanol

#increase the calculate time until 1 us#
gmx convert-tpr -s cg_md.tpr -o cg_md_1.tpr -until 1000000
gmx mdrun -s cg_md_1.tpr -v -deffnm cg_md

Analysis
#SASA#
gmx sasa -f cg_md_1.xtc -s cg_md_1.tpr -n cg_md.ndx -o 1chain_oct_sasa.xvg -or 1chain_oct_res_sas.xvg -pbc -surface -output -ndots 25

#Average#
awk '{sum+=sprintf("%f",$5)}END{printf "%.6f\n%.6f\n",sum,sum/NR}' 1chain_W_sasa.xvg

2. 1chain in water ( byrd02, 3h)
~/ProDrug/GemPi1kDa/byrd03/solution/Gem24/trajectory/1chain_water
conditions:
- 150mM NaCl + water
- 1mM ProDrug (1kda)
- 1microsecond expected
- same cg_md.itp file in octanol

Copy cg_md.xtc, cg_md.tpr, 1kda_mapped.itp from ~/ProDrug/Octanol/Take6_ok

#creat prodrug gro file#
gmx trjconv -f cg_md.xtc -s cg_md.tpr -o prodrug.gro

# Place the solute in a simulation box
gmx editconf -f prodrug.gro -bt cubic -d 1 -o prodrug_inbox.gro

# define the size of box
gmx editconf -f prodrug_inbox.gro -o system_temp.gro -d 1.0 -bt cubic -box 11.84 11.84 11.84

# Minimization in vaccum following by minimization in solution
gmx grompp -f minimization-vac.mdp -c system_temp.gro -p system.top -o minimization-vac.tpr
gmx mdrun -deffnm minimization-vac -v

# Solvatation
gmx solvate -cp minimization-vac.gro -cs water.gro -radius 0.21 -o system_W.gro

gmx grompp -f ions.mdp -c system_W.gro -p system.top -o ions.tpr

# Add ions into the box
gmx genion -s ions.tpr -p system.top -neutral -conc 0.15 -pname NA+ -nname CL- -o system_WI.gro
Then select the water group, here it’s the #3.

# Add anti-freeze water into the box
Gempi1kda 1
;W 13115
W 11533
WF 1282
NA+ 150
CL - 150

change the last 1282 W to WF in system_WI.gro

# minimization
gmx grompp -f minimization.mdp -c system_WI.gro -p system_2.top -o minimization.tpr -maxwarn 1
gmx mdrun -deffnm minimization -v

#define the set in equilibration.mdp#
vi equilibration.mdp, check the set as below;
tc-grps = ProDrug Solvent

gmx make_ndx -f minimization.gro -o system.ndx
name 2(1kda) ProDrug
3(W) | 4(WF) | 5(ION)
name 6 Solvent

# Equil
gmx grompp -f equilibration.mdp -c minimization.gro -p system.top -o equilibration.tpr -n system.ndx

gmx mdrun -deffnm equilibration -v

# Prod
gmx grompp -f dynamic.mdp -c equilibration.gro -p system.top -o dynamic.tpr -n system.ndx
gmx mdrun -deffnm dynamic -v

Analysis
#SASA#
gmx sasa -f dynamic.xtc -s dynamic.tpr -n 1chain.ndx -o 1chain_W_sasa.xvg -or 1chain_W_res_sas.xvg -pbc -surface -output -ndots 25

#Average#
awk '{sum+=sprintf("%f",$5)}END{printf "%.6f\n%.6f\n",sum,sum/NR}' 1chain_W_sasa.xvg